Specification Document Product: Rapid Flex CJ

DIVISION 3 - CONCRETE

Section 03930 - Control Joint Fillers

Part 1 – General

  - Summary

    - This section describes sealing saw-cut, control, and construction joints in concrete with a semi-rigid polyurea resin adhesive sealant, specifically SpecChem Rapid Flex CJ.

# Quality Assurance

    - Manufacturer qualifications: SpecChem must have an ongoing quality assurance program, independently audited regularly.

    - Contractor qualifications: Must have successful experience in concrete construction.

    - Comply with all safety and environmental conditions as recommended by SpecChem and local, state, and federal regulations. Refer to Safety Data Sheets (SDS) for safety and handling practices.

# Delivery, Storage, and Handling

    - Delivery: Products must arrive in original, unopened containers with labels.

    - Storage: Keep materials off the ground, protected from weather.

    - Conditioning: Follow manufacturer’s recommendations for product temperature conditioning.

# Job Conditions

    - Environmental Conditions: Apply in dry conditions with a temperature above - 20°F and rising.

    - Surface Protection: Shield all surfaces adjacent to repair areas to prevent damage and contamination.

# Submittals

    - Documentation: Provide Technical Data Sheets (TDS) and Safety Data Sheets (SDS).

# Warranty

    - Manufacturer provides a one-year warranty against material defects from the date of project completion.

# Part 2 – Products

  - Manufacturers

    - SpecChem Rapid Flex CJ, manufactured by SpecChem, conforms to this specification's requirements.

# Materials

    - Polyurea Joint Filler: Two-component, self-leveling, semi-rigid polyurea resin with a 1:1 mix ratio.

# Performance Criteria

    - Rapid Flex CJ Properties:

Pot Life: 30 Seconds Working Time: 3-4 Minutes

Cure Time: Light traffic within 1 hour, full traffic in 24 hours at 75°F Consistency: Self-leveling

Color: Standard Gray (additional colors available)

Shave Time: 20-25 minutes at 75°F

Properties when cured: Tensile Strength 1225 psi, Elongation 200%, Shore A Hardness 85.

# Part 3 – Execution

  - Surface Preparation

    - Joint Cleaning: Ensure joints are clean, dry, and free of curing compounds, densifiers, sealers, or any other foreign substances. Use a vacuum-equipped dry-cut abrasive blade and oil-free compressed air to remove water or dust before application.

    - Joint Depth: Install Rapid Flex CJ full depth in sawcut control joints and at least 2 inches deep in joints greater than 2 inches. Avoid using compressible backer rod in sawcut control joints. In construction joints, dry sand or backer rod can be used to reduce volume while maintaining a minimum 2-inch depth.

# Mixing and Application

    - Mixing Instructions: Ensure Rapid Flex CJ components are at least 50°F for mixing. Stir or shake each component before dispensing. Use a 1:1 ratio, low-pressure duplex/plural component metered pump with a 3/8” x 24” static mixer.

    - Application Process: For cartridge or plural component pump applications, dispense mixed material into a waste container first to ensure uniform color and consistent 1:1 ratio. Then, dispense properly mixed Rapid Flex CJ into the prepared joint. Overfill joints and allow to cure for about 1 hour, up to 24 hours before shaving flush with the floor using a razor scraper.

    - Curing and Shaving: Rapid Flex CJ sets quickly, reducing the risk of staining joint sides. If installed before maximum concrete shrinkage, a crack may appear, which can be refilled with Rapid Flex CJ after cleaning with SpecChem Solvent 100.

# Cleaning

    - Remove uncured material using SpecChem Solvent 100 or equivalent. Cured material must be mechanically removed.

    - Ensure cleanliness and remove any spillover from adjacent areas immediately.