# Specification Document Product: SpecFlow

Section 03 54 00 Cementitious Underlayment

# Part 1 – General

  - Summary

    - This specification outlines the application of SpecChem SpecFlow, a premium self-leveling underlayment concrete, intended for interior substrate smoothing and leveling.

# Quality Assurance

    - Manufacturer qualifications: SpecChem must have an ongoing quality assurance program, independently audited regularly.

    - Comply with all safety and environmental conditions as recommended by SpecChem and local, state, and federal regulations. Refer to Safety Data Sheets (SDS) for safety and handling practices.

# Delivery, Storage, and Handling

    - Materials delivered in original, unopened packaging. Damaged materials removed immediately. Store materials off the ground, protected from weather extremes.

# Job Conditions

    - Apply in dry conditions, above 50°F (10°C). Take measures to protect surrounding surfaces from spillage and misting.

# Submittals

    - Provide Technical Data Sheet (TDS), Safety Data Sheets (SDS), and certification of approved contractor status by SpecChem.

# Part 2 – Products

  - Manufacturer

    - SpecFlow is manufactured by SpecChem, conforming to the requirements of this specification.

# Materials

    - Primary Material: SpecFlow self-leveling underlayment.

    - Primer for Absorbent Substrates: SpecPrime, designed to enhance the bond of SpecFlow to the substrate.

    - Aggregates (if required): Clean, 3/8" pea gravel for applications exceeding 2" in thickness.

# Performance Criteria

- Compressive Strength (ASTM C109):

  - 1 Day: 3,000 psi

  - 7 Days: 4,500 psi

  - 28 Days: 5,500 psi

# Bond Strength (ASTM C882 Modified):

  - 14 Days with SpecPrime: 1,000 psi

# Flexural Strength (ASTM C348):

  - 28 Days: 1,150 psi

# Set Time (ASTM C266):

  - Initial Set: 50 minutes

  - Final Set: 80 minutes

# Yield/Density:

- Yield per Bag: 0.50 cu ft (125 lbs/cu ft)

# Application Thickness:

  - Feather edge up to 2 inches

  - Up to 5 inches with the addition of pea gravel

# Working Time:

  - Flow time: 20 minutes at 70°F

# Foot Traffic:

  - Accepts foot traffic in 2 to 4 hours depending on conditions

# Drying Time:

  - Primer drying time: 3 to 4 hours at 70°F and 50% relative humidity

# Part 3 – Execution

  - Surface Preparation

    - Cleaning the Surface: Remove dirt, grease, oil, asphalt, paint, curing compounds, and loose materials. The concrete should be profiled to a minimum CSP#3, with shot blasting preferred.

    - Priming: Apply SpecPrime at 100 - 150 sq. ft. per gallon using a brush or broom (not a roller) to ensure even coverage. Porous surfaces may require a second application. Allow SpecPrime to dry completely before proceeding with SpecFlow application.

# Mixing and Application

    - Mixing SpecFlow: Start with 4 quarts of water in a mixing container, then add one 50-pound bag of SpecFlow. Using a blending paddle attached to a heavy-duty drill (650 rpm), mix for 2 to 3 minutes until smooth and lump-free. Do not over-water or re-temper the mixture. For extended applications, add 25 pounds of clean 3/8" pea gravel per 50 pounds of SpecFlow during the last minute of mixing.

    - Application Instructions: For Interior Floors: Pour SpecFlow over the primed substrate, spreading it with a long-handled spreader or pump it for larger

areas. SpecFlow self-levels and requires no troweling. It can be applied from a feather edge up to 2" thick, and up to 5" with pea gravel. It typically supports foot traffic within 2 to 4 hours, depending on conditions. For Wood Floors: Ensure the wood subfloor is solid hardwood, at least ¾” thick, and free of flex. Prime with SpecPrime, possibly requiring two coats for porous surfaces. Install galvanized expanded metal lath mesh, stapling every 6 inches and overlapping adjacent pieces by 1 inch. Re-prime over the mesh and let dry thoroughly before applying SpecFlow.

# Finishing and Curing

    - SpecFlow self-levels and requires no grinding or sanding for a smooth finish. It is self-curing under most conditions.

# Cleaning

    - Instructions for cleaning tools and the work area with water before SpecFlow hardens, with guidelines for mechanical removal of cured material.