Specification Document Product: SpecPlug

Division 3 – Concrete

Section 03930 – Concrete Rehabilitation

# Part 1 – General

  - Summary

    - This section outlines the specifications for rapid repair of water leakage and seepage utilizing a fast-setting hydraulic-cement called SpecPlug by SpecChem.

# Quality Assurance

    - Manufacturer qualifications: SpecChem must have an ongoing quality assurance program, independently audited regularly.

    - Contractor qualifications: Must have successful experience in concrete construction.

    - Comply with all safety and environmental conditions as recommended by SpecChem and local, state, and federal regulations. Refer to Safety Data Sheets (SDS) for safety and handling practices.

# Delivery, Storage, and Handling

    - Delivery: Products should arrive in original, unopened packaging with clear labels.

    - Storage: Keep materials off the ground, protected from extreme temperatures and moisture.

    - Handling: Follow the manufacturer’s recommendations for product conditioning.

# Job Conditions

    - Environmental Conditions: Avoid application during adverse weather. Minimum temperature for application should be 40ºF and rising.

    - Protection: Guard surrounding areas against potential damage from product use.

# Submittals

    - Documentation: Provide technical data sheets, safety data sheets, and any necessary technical data.

# Part 2 – Products

  - Products

    - SpecPlug as manufactured by SpecChem must be used, adhering to this specification.

# Materials

    - Comprised of a proprietary blend of hydraulic cements and aggregates formulated for fast setting and durability.

# Performance Criteria

    - Compressive Strength (ASTM C109):

      - 1 hour: 1850 psi (12.8 MPa)

      - 1 day: 3050 psi (21.0 MPa)

      - 28 days: 7650 psi (52.7 MPa)

# Expansion (ASTM C157, moist cure):

      - 28 days: 0.08%

# Flexural Strength (ASTM C78):

      - 28 days: 1200 psi (8.3 MPa)

# Tensile Strength (ASTM C190):

      - 28 days: 800 psi (5.5 MPa)

# Set Time:

      - Initial Set: Approximately 3-5 minutes

# Color:

      - Concrete gray

# Part 3 – Execution

  - Surface Preparation

    - Enlarging Cracks: Best results are achieved by enlarging the crack to at least 3/4" in width and depth, ensuring a square or undercut shape rather than a “V” shape.

    - Cleaning: Remove all grease, wax, oil, contaminants, curing compounds, weak, contaminated, or deteriorated concrete from the substrate.

    - Wetting Surface: Saturate the repair area with water. SpecPlug can cure in the presence of running water, making it ideal for active leaks.

# Mixing and Application

    - Mixing SpecPlug: Create a putty-like consistency by adding a small amount of clean water to SpecPlug. Aim for a 20%-21% water to product ratio by weight, equivalent to about 9.5 pints of water per 50 lbs of SpecPlug. Mix enough material that can be placed within 2 minutes.

    - Application Procedure: For Vertical and Moving-Water Applications: Hold the mixed SpecPlug firmly in place until it sets, typically in about 3 minutes. Adjust water temperature to manage the setting time; use hot water and warm material to speed up the setting in cold temperatures (below 60°F) and cold water to slow down the setting in hot temperatures (above 80°F).

    - Curing: Keep SpecPlug damp for at least 30 minutes to support curing, with optimal strength achieved through wet curing for up to 2 days. This concise guide ensures the effective application of SpecPlug for stopping water flow through concrete and masonry cracks and holes. For additional information or assistance, contact SpecChem's technical support team.

# Limitations

    - Do not apply if temperatures are expected to drop below 40°F within 24 hours. Ensure proper ventilation in confined spaces.

# Cleaning

    - Remove uncured SpecPlug with water. Cured material can only be removed mechanically.