# Specification Document Product: SpecPoxy Mortar

DIVISION 3 - CONCRETE

Section 03 54 00 Concrete Restoration and Rehabilitation

# Part 1 – General

  - Summary

    - This specification outlines the application of SpecPoxy Mortar, a three-component, 100% solids epoxy mortar system designed for the repair and overlay of interior horizontal concrete surfaces.

# Quality Assurance

    - Manufacturer qualifications: SpecChem must have an ongoing quality assurance program, independently audited regularly.

    - Contractor qualifications: Must have successful experience in concrete construction.

    - Comply with all safety and environmental conditions as recommended by SpecChem and local, state, and federal regulations. Refer to Safety Data Sheets (SDS) for safety and handling practices.

# Delivery, Storage, and Handling

    - Ensure all materials are delivered in their original, unopened packaging, labeled with content identification, batch numbers, and expiration dates. Inspect materials for damage upon arrival.

    - Store materials in a dry, well-ventilated area between 45°F and 95°F. Protect from direct sunlight and moisture.

    - Handle products according to SpecChem’s recommendations to avoid contamination and ensure product integrity.

# Job Conditions

    - Application Conditions: Do not apply if the substrate and ambient temperatures are below 50°F. Ensure the substrate is dry and free from standing water or ice.

    - Surface Protection: Take measures to protect adjacent areas from spillage and overspray. Provide adequate ventilation in confined areas.

# Submittals

    - Submit manufacturer's technical data sheets, including installation instructions, SDS, and material warranty information.

# Part 2 – Products

  - Materials

    - Main System: SpecPoxy Mortar Kit, pre-measured for proper proportioning of resin, hardener, and aggregate.

    - Performance Criteria: Conform to ASTM (C881, Type III, Grade I) standards for epoxy mortar systems, ensuring high tensile, compressive, and flexural strengths suitable for industrial and commercial flooring.

# Performance Criteria

    - Compressive Strength (ASTM C579):

      - 9,600 psi

# Bond Strength (ASTM C882):

      - 2,650 psi

# Tensile Strength (ASTM C307):

      - 1,650 psi

# Flexural Strength (ASTM C580):

      - 3,450 psi

# Hardness (ASTM D2240, Shore D):

      - 85

# Water Absorption (ASTM D570):

      - Less than 0.5%

# Part 3 – Execution

  - Surface Preparation

    - Cleaning the Surface: Ensure all surfaces are clean, dry, and free from oil, grease, dirt, laitance, curing compounds, and other foreign materials. Mechanical abrasion or sandblasting is recommended to remove contaminants and create a profile suitable for bonding.

# Mixing and Application

    - Mixing Instructions: Ensure air, material, and surface temperatures are between 50°F and 90°F. Precondition materials to approximately 70°F for easier mixing. Mix components separately before combining. Mix one part of component A with one part of component B by volume for 2-3 minutes using a low-speed drill and Jiffy mixer or paddle. Mix only as much material as can be used within the product's pot life. Gradually add part C (aggregate) to the mixed components A and B, ensuring all aggregates are thoroughly coated with the epoxy resin.

    - Placing the Mortar: Apply the mixed epoxy mortar immediately, or within 30-40 minutes, to the prepared surface using a trowel or rake. Use SpecChem Solvent 100 as a finishing aid to lubricate the trowel for a smooth finish. For increased texture and improved traction, broadcast additional dry sand into the wet mortar immediately after application.

# Coverage and Curing

    - The coverage rate for a 1/2 cubic foot unit at a 1/4” thickness is approximately 24 sq-ft.

    - SpecPoxy Mortar cures to a light gray mortar color, ready for foot traffic in 12 hours and vehicle traffic in 24 hours.

# Cleaning

    - Clean tools and equipment immediately with an appropriate solvent before the material hardens. Dispose of waste according to local, state, and federal regulations.